SRP AirOutshield Inc.

SRP AirOutshield™ ROOF

Email: info@SRPAirOut.com

URL:  www.srpairoutshield.com

Revision date: April 2025

SPEC NOTE: This specification is a guide only and may need editing for the specific intended application. It is the responsibility of the design professional to ensure the accuracy and completeness of the specifications issued. SRP AirOutshield ROOF is not recommended for roofs with a slope of less than 2:12.

GENERAL

SUMMARY

Section includes: exterior roof, vapor permeable underlayment.

Related Sections include the following:

Division 6 Section "Rough Carpentry" for exterior sheathing.

Division 7 Section ["Clay Tile"] ["Wood Shakes and Shingles"] ["Metal Roofing"] for roofing assembly.

Division 13 Section "Pre-Engineered Buildings" for metal siding and roofing.

REFERENCES

ASTM International (ASTM)

ASTM D226: Standard Specification for Asphalt-Saturated Organic Felt Used in Roofing and Waterproofing

ASTM D1970: Standard Specification for Self-Adhering Polymer Modified Bituminous Sheet Materials Used as Steep Roofing Underlayment for Ice Dam Protection

ASTM D4869: Standard Specification for Asphalt-Saturated Organic Felt Underlayment Used in Steep Slope Roofing

ASTM E84: Standard Test Method for Surface Burning Characteristics of Building Materials ​

ASTM E96: Standard Test Methods for Water Vapor Transmission of Materials

SUBMITTALS

Product Data: Include manufacturer's written instructions, technical data, and tested physical and performance properties of breathable underlayment.

Shop Drawings: Provide drawings showing relationship of underlayment to:

Framing or blocking members.

Purlins.

Metal Decking.

Thermal Insulation.

Sheathing.

All roofing, fascia and gable end conditions.

Roofing or attic ventilation penetrations.

Roof curbs.

Pipe, Conduit and Duct penetrations.

Include actual manufactured flashing and or “weather-heads.”

Samples:

8-1/2 inch-x-11-inch (216mm x 280mm) square of breathable underlayment sheet.

Tapes (Single & Double-Sided).

Provide materials and fasteners for mock-up

Manufacturer’s Instructions: Provide manufacturer’s instructions showing the recommended procedures and sequence of installation of breathable underlayment.

QUALITY ASSURANCE

Ensure all work of this section and the related sections is performed in accordance with local codes and system manufacturer’s instructions.

Obtain all breathable underlayment through one source from a single manufacturer.

Pre-installation Conference: Conduct conference at Project site to comply with requirements in Division 1 Section "Project Management and Coordination." Review requirements for underlayment, including surface preparation specified under other Sections, substrate condition and pretreatment, temporary weather protection, forecasted weather conditions, special details and sheet flashings, installation procedures, testing and inspection procedures, and protection and repairs.

Mock-Up:

Prior to installing the main roof underlayment, install mock-up on site at location directed by Architect.

Mock-up Size: Minimum 4 feet x 4 feet (1.2 m x 1.2 m).

Mock-up Scope: Demonstrate substrate preparation, underlayment application, horizontal and vertical laps, fastening method, sealing of typical penetrations and edge termination at eave or rake.

Review: Obtain Architect approval of mock-up for workmanship, adherence to details, and compliance with manufacturer's instructions before proceeding with general installation.

Approved mock-up [may remain as part of the Work] [shall be removed after acceptance].

DELIVERY, STORAGE, AND HANDLING

Deliver materials to Project site in original containers with seals unbroken, wrapped in a polythene sleeve, labeled with manufacturer's name, and product brand name.

Store rolls under cover, on a clean, level surface, either flat or upright.

- PRODUCTS

MANUFACTURERS

Acceptable Product: SRP AirOutshield™ ROOF by SRP AirOutshield Inc., telephone 1-866-533-0233, website www.SRPAirOutshield.com

Substitutions: Submit requests for review in accordance with Section 01 25 00 – Substitution Procedures.

MATERIALS

Air Barrier Underlayment: Triple-layer, spun-bonded polypropylene membrane designed for use as a water-resistant, vapor-permeable air barrier underlayment on sloped roofs.

Performance Requirements:

Nominal weight: 5.0 oz/yd² (170 g/m²).

Nominal thickness: 1/32 in (0.6 mm).

Water vapor transmission (ASTM E96 - Procedure A): 119 perms (6,808 ng/Pa·s·m²)

Tensile strength:

Machine direction: 188 lb/in (330 N/50 mm).

Cross direction: 143 lb/in (250 N/50 mm).

Service temperature range: -40 °F to 212 °F (-40 °C to 100 °C).

Flame Spread Rating (ASTM E84):

Flame Spread Index: 5.

Smoke Developed Index: 5

UV resistance: Withstand exposure up to 120 days prior to covering.

Pliability: Pass to ASTM D226.

Aging resistance: Pass to AC48 Section 4.7.

Liquid water transmission: Pass to ASTM D4869.

Low/High temperature unrolling: Pass to ASTM D1970.

Physical Characteristics:

Roll dimensions: 59 in x 164 ft (1.5 m x 50 m).

AUXILIARY MATERIALS

Seam Seal Tape:

SRP 60 UV Tape distributed by SRP AirOutshield Inc

SRP 100 UV Tape distributed by SRP AirOutshield Inc

SRP 1” D.S (double sided) Tape distributed by SRP AirOutshield Inc

Eave Protection: Self adhered membrane.

High Temperature resistant underlayment complying with ASTM D1970, rated for high-temperature applications with minimum service temperature of 240°F suitable for use under specified primary roofing.

Fasteners

Fasteners: Minimum No. 12-gage [0.109-inch-shank-diameter (2.77mm)] corrosion-resistant steel or stainless steel nails having a minimum 3/8-inch diameter (9.5 mm) head, or minimum No. 14 gage [0.083-inch-shank-diameter (2.11 mm)] corrosion-resistant steel or stainless steel screws or nails installed with a 1-inch-diameter (25.4 mm) caps, plate or washer.

Ventilation Mat: non-woven nylon with maximum 20% or battens over underlayment as indicated on Drawings.

- EXECUTION

EXAMINATION

Examine substrates, areas, and conditions, with Installer present, for compliance with requirements and other conditions affecting performance.

Refer to the most recent version of the manufacturer’s installation guide as available at srpairoutshield.com

SURFACE PREPARATION

Clean and prepare substrate according to manufacturer’s written recommendations. Provide clean and dry substrate free of frost, loose nails, dirt, debris or other containments that would adversely affect the installation of the breathable underlayment.

Do not expose the membrane to chemicals including surfactants, soaps and solvents.

PENETRATIONS

Seal all penetrations using AirOutshield ROOF in combination with SRP Tapes, Self adhered membranes and other compatible sealants and products.

Pipes and Conduit:

Install manufactured penetration sleeves sized for the penetration and install as recommended by the manufacturer.

Unroll SRP AirOutshield ROOF membrane next to penetration and fold membrane back on itself. Mark and cut out penetration size out of membrane. Ensure cutout section is slightly smaller than diameter of penetration. Slide membrane over penetration.

Wrap SRP 100 UV Tape around penetration. Ensure that 2 inch (51mm) extends onto the membrane. If required, install a second 4 inch (100 mm) piece of SRP 100 UV Tape around the penetration. Refer to manufacturer’s standard details.

Large, Curbed, Roof Penetrations:

Follow roof manufacturers and curb manufacturer’s approved shop drawings for curb and roof system installation.

BREATHABLE UNDERLAYMENT APPLICATION

SRP AirOutshield ROOF is installed as a secondary drainage plane under the primary water shedding roofing such as tile, slate, zinc, copper or metal roofing material.

Install printed side up, laid such that it forms a continuous membrane over the entire roof area, allowing any water to drain down to the gutters. Avoid blockages that would otherwise obstruct the water flow.

Do not use on roofs with slope less than 2:12 (16.7 %).

Fasten using roofing nails, screws or other approved fastener. Do Not use Staples. Ensure compatibility between fasteners and the roofing material.

Mechanical fasteners that penetrate the AirOutshield ROOF must be set flush and fastened securely into solid backing. When fastening into gypsum board and other non-structural boards, ensure the fastener penetrates a stud or other solid backing.

Take appropriate precautions during installation in high winds to avoid injury.

Along valleys, hips and ridges, install eave protection membrane and ensure overlap minimum 12 inch (305mm) o.c. both sides.

Where the self-adhered membrane is to be applied over SRP AirOutshield ROOF do not apply primers as they will damage the AirOutshield.

At eaves, install SRP AirOutshield ROOF overlapping the self-adhered eave protection membrane by 12 inches (305mm) minimum.

Unroll SRP AirOutshield ROOF horizontally across the roof perpendicular to roof slope. Install successive layers of SRP-AirOutshield ROOF in a shingling manner up the roof slope maintaining minimum 6” horizontal and vertical overlaps.

Tape all seams using SRP 60 UV Seam Seal Tape when roof slope is 3:12 or less or as required by the project specification

SPEC NOTE: The following paragraph is optional and required if the system must be installed as an air barrier.

To make the AirOutshield ROOF the deemed air barrier, tape all vertical and horizontal seams using SRP 60 UV Seam Seal Tape.

Extend AirOutshield ROOF 4 inch (100 mm) over gable ends and fasten to fascia boards at 305mm (12 inch) o.c.

Fasten AirOutshield ROOF along top and bottom of roll at 12 inch (305mm) o.c. and maximum 24 inch (610 mm) o.c. in the field.

During installation, protect SRP-AirOutshield ROOF from rainwater runoff from upper to lower roofs (overhangs/eaves/valleys).

Limit heavy foot traffic on SRP-AirOutshield ROOF and repair any damaged material due to traffic abuse.

Roof Installation:

Ensure SRP-AirOutshield ROOF is installed in compliance with this specification and all details are complete.

SPEC NOTE: The following paragraph is optional and required if the system must be installed with a ventilation mat.

Install Ventilation Mat or battens over the SRP AirOutshield ROOF to form a positive drainage and ventilation space.

Install primary roofing system as soon as possible and in accordance with the roof system manufacturers written instructions and the project specifications.

FIELD QUALITY CONTROL

[Owner will engage] [Engage] an independent inspector to observe substrate and installation. Inspector shall provide a written, sign-off log, on all penetrations before the underlayment is placed against them. Form of log shall be approved by Architect before contract with inspection service is approved.

PROTECTING AND CLEANING

Protect installed SRP AirOutshield ROOF from damage due to ultraviolet light, harmful weather exposures, physical abuse, exposure to solvents or soaps and other causes. Augment SRP AirOutshield ROOF with additional waterproofing materials (e.g., tarps) DURING THE CONSTRUCTION PHASE to ensure that interiors are protected until the primary roofing material is applied.

Repair torn breathable underlayment as follows:

Insert a full height piece of underlayment extending 12 inch (305mm) horizontally beyond the damage and extend up and under the underlayment above. Mechanically attach underlayment to substrate top and bottom. Tape all seams.

Remove mud and similar marks with a water scrub; do not use soap or solvents. If chemicals have been spilled on underlayment, remove and replace as stated above.

END OF SECTION